### Coir Mat 70 Technical Specifications

| Property | Test Method | Details |
| --- | --- | --- |
| Dry Tensile Strength | ASTM D 4595 | Machine Direction 1,512 lbs./ft. (22.06 kN/m) Cross Direction 1,032 lbs./ft. (15.05 kN/m) |
| Wet Tensile Strength | ASTM D 4595 | Machine Direction 924 lbs./ft. (13.48 kN/m) Cross Direction 684 lbs./ft. (9.97 kN/m) |
| Elongation at Failure Wet | ASTM D 4595 | Machine Direction 69% Cross Direction 34% |
| Thickness | ASTM D 5199 | 0.35 in (9 mm) |
| UV Stability | ASTM D 4355 | 80% min @ 500 hrs |
| Open Area | Measured | 50% |
| Recommended Slope | Observed | 2:1 or 1:1 |
| Recommended Flow | Flume Tests | 12 fps (3.7 m/s) |

### Coir Erosion Mat Roll Sizes

| Roll Size | Total Area |
| --- | --- |
| 6.56 ft x 165 ft (2 m x 50 m) | 120 SY/roll (100 m²/roll) |
| 13.1 ft x 165 ft (4 m x 50 m) | 240 SY/roll (200 m²/roll) |
| 13.1 ft x 83 ft (4 m x 25 m) | 120 SY/roll (100 m²/roll) |