Division 400 of the Standard Specifications for Highway Construction, Edition of 2014, is hereby amended as follows:

The fourth sentence of Paragraph 1 of Subsection 404.01(b), Design Requirements, is hereby deleted and the following substituted therefor:

The optimum asphalt content is the asphalt binder content at 4% Air Voids (AV).

The first bullet of Paragraph 1 is hereby deleted and the following substituted therefor:

- PG 64-22 and PG 70-22 mixes will be designed using 4% air voids;

The second sentence of Paragraph 2 of Subsection 404.04, Quality Control of Asphalt Mixtures, is hereby deleted and the following substituted therefor:

Adjustments to the accepted mix design to conform to actual production values without re-design of the mixture shall be based on production of the mixture at a target value of 4.0% Air Voids (AV) in specimens and an asphalt binder content not less than that specified in the accepted mix design.

Table 405-1 of Subsection 405.03 Materials is hereby deleted and the following substituted therefor:

| Table 405-1 |  |  |  |
| --- | --- | --- | --- |
| Design Requirements for Asphalt Concrete Hot Mix Base Course (1-1/2″ [37.5 mm]) |  |  |  |
|  | Control Points |  |  |
| Sieve (mm) | Percent Passing (%) |  |  |
| 2″ (50.0) | 100 |  |  |
| 1½″ (37.5) | 90 - 100 |  |  |
| 1″ (25.0) | 90 max. |  |  |
| No. 4 (4.75) | - |  |  |
| No. 8 (2.36) | 15 - 41 |  |  |
| No. 16 (1.18) | - |  |  |
| No. 30 (0.60) | - |  |  |
| No. 50 (0.30) | - |  |  |
| No. 200 (0.075) | 0 - 6 |  |  |
| Asphalt Binder Content |  | Design Value |  |  |
| % Air Voids |  | 4.0 |  |  |
| % VMA |  | 11.5 – 13.0 |  |  |
| Minimum Water Sensitivity Ratio |  | 80.0 |  |  |
| % Anti-strip |  | As Required |  |  |
| Fines to Asphalt Ratio* |  | 0.6 – 1.6 |  |  |
| # Wheel Tracking Test (8000 cycles, 100 psi, 64ºC) |  | Design Gyration Maximum Rut 75 & 115 0.315 in. (8.000 mm) 160 0.197 in. (5.000 mm) 205 0.197 in. (5.000 mm) |  |  |

*Fines to asphalt ratio shall be defined as the percent materials passing the No. 200 (0.075 mm) sieve (expressed as a percent of total aggregate weight) divided by the effective asphalt binder content.

Table 406-1 of Subsection 406.04, Construction Requirements and Acceptance, is hereby deleted and the following substituted therefor:

| Table 406-1 |  |  |  |
| --- | --- | --- | --- |
| Design Requirements for Asphalt Concrete Hot Mix Binder Course (1″ [25 mm]) |  |  |  |
|  | Control Points |  |  |
| Sieve (mm) | Percent Passing (%) |  |  |
| 1½″ (37.5) | 100 |  |  |
| 1″ (25.0) | 90 - 100 |  |  |
| ¾″ (19.0) | 90 max. |  |  |
| No. 4 (4.75) | - |  |  |
| No. 8 (2.36) | 19 - 45 |  |  |
| No. 16 (1.18) | - |  |  |
| No. 30 (0.60) | - |  |  |
| No. 50 (0.30) | - |  |  |
| No. 200 (0.075) | 1 - 7 |  |  |
| Asphalt Binder Content |  | Design Value |  |
| % Air Voids |  | 4.0 |  |
| % VMA |  | 12.5 – 14.0 |  |
| Minimum Water Sensitivity Ratio |  | 80 |  |
| % Anti-strip |  | As Required |  |
| Fines to Asphalt Ratio* |  | 0.6 – 1.6 |  |
| Wheel Tracking Test (8000 cycles, 100 psi, 64ºC) |  | Design Gyration Maximum Rut 75 & 115 0.315 in. (8.000 mm) 160 0.197 in. (5.000 mm) 205 0.197 in. (5.000 mm) |  |

*Fines to asphalt ratio shall be defined as the percent materials passing the No. 200 (0.075 mm) sieve (expressed as a percent of total aggregate weight) divided by the effective asphalt binder content.

Table 407-1 and Table 407-2 of Subsection 407.04, Construction Requirements and Acceptance, are hereby deleted and the following substituted therefor:

| Table 407-1 |  |  |  |
| --- | --- | --- | --- |
| Design Requirements for Asphalt Concrete Hot Mix Surface Course (1/2″ [12.5 mm]) |  |  |  |
|  | Control Points |  |  |
| Sieve (mm) | Percent Passing (%) |  |  |
| ¾″ (19.0) | 100 |  |  |
| ½″ (12.5) | 90 - 100 |  |  |
| 3/8″ (9.5) | 90 max. |  |  |
| No. 8 (2.36) | 28 - 58 |  |  |
| No. 16 (1.18) | - |  |  |
| No. 30 (0.60) | - |  |  |
| No. 50 (0.30) | - |  |  |
| No. 200 (0.075) | 2 - 10 |  |  |
| Asphalt Binder Content |  | Design Value |  |
| % Air Voids |  | 4.0 |  |
| % VMA |  | 14.0 – 16.0 |  |
| Minimum Water Sensitivity Ratio |  | 80.0 |  |
| % Anti-strip |  | As Required |  |
| Fines to Asphalt Ratio* |  | 0.6 – 1.6 |  |
| Wheel Tracking Test (8000 cycles, 100 psi, 64ºC) |  | Design Gyration Maximum Rut 75 & 115 0.315 in. (8.000 mm) 160 0.197 in. (5.000 mm) 205 0.197 in. (5.000 mm) |  |

*Fines to asphalt ratio shall be defined as the percent materials passing the No. 200 (0.075 mm) sieve (expressed as a percent of total aggregate weight) divided by the effective asphalt binder content.

| Table 407-2 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Design Requirements for Asphalt Concrete Hot Mix Surface Course (3/8″ [9.5 mm]) |  |  |  |  |
|  | Control Points |  |  |  |
| Sieve (mm) | Percent Passing (%) |  |  |  |
| ½″ (12.5) | 100 |  |  |  |
| 3/8″ (9.5) | 90 - 100 |  |  |  |
| No. 4 (4.75) | 90 max. |  |  |  |
| No. 8 (2.36) | 32 - 67 |  |  |  |
| No. 16 (1.18) | - |  |  |  |
| No. 30 (0.60) | - |  |  |  |
| No. 50 (0.30) | - |  |  |  |
| No. 200 (0.075) | 2 - 10 |  |  |  |
| Asphalt Binder Content |  |  | Design Value |  |
| % Air Voids |  |  | 4.0 |  |
| % VMA |  |  | 15.0 – 17.0 |  |
| Minimum Water Sensitivity Ratio |  |  | 80.0 |  |
| % Anti-strip |  |  | As Required |  |
| Fines to Asphalt Ratio* |  |  | 0.6 – 1.6 |  |
| # Wheel Tracking Test (8000 cycles, 100 psi, 64ºC) |  | Design Gyration Maximum Rut 75 & 115 0.315 in. (8.000 mm.) 160 0.197 in. (5.000 mm) 205 0.197 in. (5.000 mm) |  |  |

*Fines to asphalt ratio shall be defined as the percent materials passing the No. 200 (0.075 mm) sieve (expressed as a percent of total aggregate weight) divided by the effective asphalt binder content.